Synthesis and Applications of Biodegradable Polymers – A Review

Trina Dutta1, Souvik Chatterjee2, Manabi Ghosh3, Sangita Bhattacharjee4*

1Assistant Professor, Department of Chemistry, JIS College of Engineering, Kalyani, West Bengal, 741235

2,3UG Student, Department of Chemical Engineering, Heritage Institute of Technology, Kolkata – 700107

4Assistant Professor, Department of Chemical Engineering, Heritage Institute of Technology, Kolkata – 700107

*Sangita Bhattacharjee, sangita.bhattacharjee@heritageit.edu, +91-9874529845,

Green Chemistry and Environment:

Abstract

Disposal of petroleum derived polymers such as polyethylene, polypropylene, and polyvinyl chloride has severe environmental impact as burning of these non-biodegradable materials causes  global warming problem resulting from carbon dioxide emission. Researches have been carried out across the globe to produce biodegradable polymers which can replace non – biodegradable petro-polymers. Petro polymers, due to lack of complete recycling system and inadequately managed garbage system, ultimately end up in seas and oceans where these get converted to micro-plastic and macro plastics and ultimately enter in the food web. Biodegradable polymers, due to bio-compatibility and ability to be broken down into natural components, are nowadays being applied in medical, packaging as well as in agricultural fields. Biodegradable polymers can be synthesized from bio wastes or bio-resources which are renewable sources. Biopolymers such as cellulose, chitosan and starch are extracted from agricultural-waste and vegetable oil, fats, cellulose, starch from food waste. Biopolymers such as poly lactic acid, polyhydroxyalkanoates can be produced from polysaccharides, complex sugars and fatty acids of bio-waste through fermentation and subsequent polymerization route. These biopolymers when disposed to environment degrade to yield water, carbon dioxide, methane, humic acid and other natural components. To increase the use of biopolymer, extensive researches  have been carried out globally to enhance physical and mechanical properties of biopolymers at par to those of petro polymers.

Keywords: Global warming; bio-compatibility; environment

1.0 Introduction

Plastics, a large family of polymers, derived from petroleum have a broad range of properties. Due to their cost, durability, strength to weight ratio etc. they are extensively used in daily life. However due to their non-biodegradability, single use and durability, plastic fraction in municipal solid waste are showing increasing trend. By 2050, it is predicted that globally, oil consumption on account of plastic production will rise from present 4 – 8% to 20%. The problem of huge quantity of accumulation of plastic, a persistent pollutant has, caused severe environmental threat across the globe due to production and consumption in enormous quantities. As per recent study,  plastic use is expected to rise from 464 Mt in 2020 to 884 Mt in 2050 and reach an  accumulation of 4754 Mt in 2050 (from the year 2020) [1SB.]. As garbage disposal and segregation systems are not satisfactory, the waste plastic is improperly discarded and thus got leached in ecosystem. A substantial quantity of plastics end up as plastic debris in sea bed as well as surface of ocean and seas. Ocean waves and UV radiation convert the macro plastic to micro plastic which has a size range of 1 µm to 5 mm. As several marine species such as sea-reptiles, mussels, plankton and fishes consume these microplastics as these float with currents, microplastics accumulate, magnify and propagate to higher trophic levels. The ingested plastic cause a lot of health problems in animals. Due to very low degradation rates, macro, micro and nano plastics tend to accumulate in off-shore, on shore and coastal region as persistent organic pollutant. In these context, biodegradable plastics, produced from renewable, natural sources can be the best alternatives.

2.0 Applications

Bioplastics or alternative to petroleum based plastics are made of natural materials, so these are biodegradable in nature. Hence they provide environment friendly alternative for packaging and products. Nowadays petroleum based disposable plastic articles such as cups, straws, cutlery, containers are getting replaced by various types of bioplastics at a low but steady pace across the globe. Some of the biobased plastics are biodegradable that means these decompose in less than a year when exposed to naturally occurring bacteria, algae and fungi. Few biodegradable plastics may be compostable which means that within a span of three months they will completely decompose to nutrient-rich biomass [2SB].  Some biodegradable plastic may degrade within 20-45 days forming carbon dioxide, water, biomass, methane and inorganic compounds if required environmental conditions and microorganisms are available whereas petrochemical plastics require 100-1000 years to degrade thereby causing huge accumulation of plastics [3,4SB]. Recent research has shown that [5SB] Aeromicrobium sp. JJY06, a new isolated strain can degrade three commercial bioplastics such as ε- polycaprolactone (PCL), poly butylene succinate (PBS) and poly butylene adipate-co-terephthalate (PBAT)  even at low temperatures [[5SB].

Biodegradable polymers have certain limitations such as relatively high cost, low mechanical strength and different thermochemical properties than conventional plastics. Glass and carbon fibers, are blended with the biopolymer to overcome those limitations, but these are also not biodegradable. To improve mechanical strength, rigidity and thermal resistance, micro and nano sized natural materials such as bentonite, calcium carbonate, alumino-silicate and natural fibers such as lignocellulosic fibers, wood fibers etc. are incorporated in the bio-polymer as filler [6SB].

Due to high tensile strength and heat tolerance, starch based bioplastic may be incorporated with petro-polymer or biopolymer to produce novel composite material. According to some market survey report, out of 2.05 million tons of bioplastics manufactured in the year 2017, 18.8% of it is accounted for starch blend. From starch-based compostable plastics, the Green Dot Bioplastic team has successfully manufactured cell-phone cases [7SB]. Research is going on to explore usage of starch-based plastic composite in  packaging field, food service disposables, compostable kitchen bags etc. [7 SB]. Cellulose based bioplastics, derived from cellulose ester and other derivatives are used in extruded films, molding materials, electronics, rods, eyeglass frames etc. Protein based bioplastics are derived from plant and animal protein such as gluten, soy, whey casein etc. These are used as edible film used in food packaging, coatings for fruits and vegetables, as biodegradable mulch film, plant pots, in medical field as surgical films and drug delivery system as well as in consumer goods such as cosmetic containers etc. By incorporation of different biopolymers such as gelatin and saccharose to the protein based polymer or by using various crosslinking methods, an improvement of mechanical properties, stiffness and decrease of water absorption capacity and deformability can be achieved. Produced from agricultural waste products, these types of bioplastic offers sustainable development and strengthen circular economy concept.

Biodegradable and bio-based thermoplastic poly lactic acid (PLA), due to its versatility, biocompatibility, compostability and oil resistance  are mainly used as food containers, bags, garbage disposable cutlery. PLA is an aliphatic polyester which can be biodegraded under suitable composting environment involving microbial activity, elevated temperature and moisture content resulting hydrolytic cleavage of reducing molecular weight prior to complete biodegradation. PLA  is one of the most popular material for rapid prototyping 3D printing, low warping and ease of use. PLA also used for consumer items including furniture component and toys and for fibers in carpets and clothes in textile industries. PLA fiber is popular as it is light weight, skin-friendly, warm and breathable and less costly than some of synthetic fibers.It is used to produce woven disposable cloths, diapers and feminine hygiene products. Because of its biocompatibility, PLA is used in drug delivery systems, orthopedic implants and tissue engineering scaffolds. In specialized applications, PLA composites are reinforced with nanoparticles to improve thermal stability, strength and antimicrobial property [6SB].

Polyhydroxyalkanoates (PHA), polyhydroxy esters of 3-,4-, 5- and 6-hydroxy alkanoic acids, are biodegradable, non-toxic, bio-compatible polymers. Depending upon chain lengths, PHA s are categorized in short chain (scl-PHA) containing 3-5 carbon atoms in a monomer, medium chain length containing 6 – 14 carbon atoms in a monomer and long chain length (lcl-PHA) containing 15 or more carbon atoms in a monomer. PHAs can be modified to be used in packaging, agriculture, molding products, adhesives, films, paper coatings, drinking straws, packaging materials, diapers, milk cartons, shampoo bottles etc. due to its water resistance property. Due to  bio-compatibility of PHAs, these are used as implant materials, stents, orthopedic pins, cardiac valves articular cartilage devices and patches, wound dressing etc. PHA is used to form agricultural mulch films used to retain soil integrity, weed control and moisture retention [8,9 SB].

Polyhydroxybutyrate (PHB) is the rigid type biopolymer within the PHA family, it is classified as short-chain-length PHA, consisting monomers of 3-hydroxybutyrates . These are stiff, brittle and hence often are used in rigid packings. These are also used in biomedical applications. In some study by Bissery et al. in 1985, microspheres of anticancer drug, lomustine have been prepared using PHB and PLA respectively. Report revealed that PHB facilitates rapid release of the drug compared to PLA [10SB].  PHB has certain restrictions poor thermal stability, slow crystallization, brittleness and poor melt processability. The functionality of PHB can be improved by co-polymerized HB with hydroxyvalerate (HV) to form the resulting copolymer PHBV( Poly(3-hydroxybutyrate-co-3-hydroxyvalerate) ). Due to higher tensile strength, toughness, stiffness, excellent film-forming capability and biocompatibility, PHBV, the linear aliphatic polyester,  is suitable for specialty packaging and in medical application such as controlled drug release system, orthopedic devices etc.

References:

# Tanja Narancic, Federico Cerrone, Niall Beagan, Kevin E O’Connor, ‘Recent Advances in Bioplastics: Application and Biodegradation’, Polymers, 2020, Apr 15;12(4):920. doi: 10.3390/polym12040920

- https://www.greenbusinessbenchmark.com/archive/5-bioplastic-types#

- Wang J, Tan Z, Peng J, Qiu Q, Li M (2016) The behaviors of microplastics in the marine environment.Mar Environ Res 113:7–17

- Ghimire S, Flury M, Scheenstra E, Miles C (2020) Sampling and degradation of

biodegradable plastic and paper mulches in field after tillage incorporation. Sci Total Environ 703:135577

- Geeta Chhetria1, Jong-MinJeona1, Gayeon Hwanga, Tae-Rim Choia, Yung-HunYangb, Chang-JunChac, Jeong-JunYoon, Biodegradation of PCL, PBS, and PBAT at low temperatures by Aeromicrobium sp. JJY06: A newly isolated strain for cold-environment plastic cleanup, 2025, Journal of Hazardous Materials, vol. 495, Sept. 2025, 138896

- Oznur Kaya Cakmak, ‘Biodegradable Polymers—a Review on Properties, Processing, and Degradation Mechanism’, Circular Economy and Sustainability (2024) 4:339–362, https://doi.org/10.1007/s43615-023-00277-y.

- https://www.greendotbioplastics.com/starch-based-plastics/

- Antony V Samrot et al., The Synthesis, Characterization and Applications of Polyhydroxyalkanoates (PHAs) and PHA-Based Nanoparticles’ Polymers, 2021 Sep. 27;13(19):3302. doi: 10.3390/polym13193302

- Gupta, S., Sharma, S., Kumar, A., Saad, M., Husain, B., Gupta, A., 2022. Materials Today : proceedings Biopolymers from waste biomass and its applications in the cosmetic industry : a review. Mater. Today: Proc. https://doi.org/10.1016/j. matpr.2022.06.422

- https://www.sciencedirect.com/topics/agricultural-and-biological-sciences/polyhydroxybutyrate